THE UNIVERSITY OF ZAMBIA

SCHOOL OF ENGINEERING

DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING

CEE 3111 – CIVIL ENGINEERING MATERIALS AND CONSTRUCTION PRACTICES

LAB No:

TITLE:

NAME:

COMPUTER No:

DATE DUE:

ATTENTION:

1

## TENSION TEST OF STEEL AND ALUMINUM

MUBANGA NTENDA

2016144272

MR. L.H KAMISA

# IMPORTANCE

The parameters obtained from this test can be used to determine the stress-strain relation of a metal and such information is important for alloy development, design, quality control and comparison of different sets of metals.

# PROCEDURE

Having specifically worked with the aluminum specimen, an aluminum bar 500mm long with diameter 10mm was measured using a ruler and the center identified after which 25mm offsets where marked on either side of the center to determine the gauge length. The marked bar was placed uniaxially on the universal testing machine. The machine was set to ‘tension’ and the test was initiated until the aluminum specimen reached the point of fracture. The final gauge length and the diameter at the neck was measured and recorded.

# RESULTS

The following table shows the raw data obtained in the experiment:

|  | Aluminum | Steel (Deformed Bar) | Steel (Round Bar) |
| --- | --- | --- | --- |
| Initial Length (mm) | 500 | 500 | 500 |
| Final Length (mm | 615 |  |  |
| Initial Gage Length (mm) | 50 | 50 | 50 |
| Final Gage Length (mm) | 60 |  |  |
| Initial Diameter (mm) | 10 | 10 | 10 |
| Final Diameter (mm) | 3.10 |  |  |
| Initial Area (mm2) | 78.540 | 78.540 | 78.540 |
| Final Area (mm2) | 7.55 |  |  |

The following table shows the derived data after performing the tensile test on the respective specimens:

|  | Aluminum | Steel (Deformed Bar) | Steel (Round Bar) |
| --- | --- | --- | --- |
| Yield Strength (MPa) | 77.05 | 590.5 | 406.1 |
| Tensile Strength (MPa) | 112.671 | 683.64 | 592.2 |
| Rapture Strength (MPa) | 108.32 | 680.32 | 588.3 |
| Elasticity Modulus (GPa) | 14.5 | 62.9 | 93.7 |
| Elongation (mm) | 10 |  |  |
| %Reduction of Area | 90.4 |  |  |

# DATA ANALYSIS

## STRESS-STRAIN CURVES

- ALUMINIUM:

- HIGH YIELD STEEL (DEFORMED BAR)

- MILD STEEL (ROUND BAR):

# DISCUSSION

# CONCLUSION