## Slide 1
GMM 2110: Introduction to Geology Mining and Metallurgy
By
Marthias SILWAMBA (PhD)
Metallurgical Engineering Department
Marthias.silwamba@unza.zm

## Slide 2
Lecture 5
Introduction to mineral concentration and dewatering
MS© 2021

## Slide 3
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 4
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 5
5.1. Introduction
MS© 2021
Liberated minerals
Valuable mineral concentration
Froth flotation
Magnetic separator
Electrical separator
Gravity separator
jigging
Spiral
Shaking table
Dense media
Valuable minerals are concentrated by separation from the gangue minerals using various techniques.

## Slide 6
5.1. Introduction (cont.)
MS© 2021
Separation methods and the physical properties utilized to achieve seperation (concentration).
Separation methods | Physical property for separation | Particle size [cm]
Gravity separation (Jig) | Density | 0.5-200
Gravity separation (Air table) |  | 0.5-50
Gravity separation (Shaking table) |  | 0.05-1
Dense medium separation |  | 0.5-300
Magnetic separation | Magnetism | 0.15-200
Eddy current separation | Electrical conductivity | 5-40
Electrostatic separation |  | 0.1-4
Flotation | Surface wettability | 0.005-0.5

## Slide 7
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 8
Froth flotation utilises the difference in physico-chemical surface properties of particles of various minerals.
In other words, flotation separates materials based on the differences in surface wettability.
To enhance the differences in surface wettability, particles are treated with reagents, and, for flotation to take place, an air-bubble must be able to attach itself to a particle, and lift it to the water surface.
5.2. Froth flotation fudamentals
MS© 2021
B: hydrophilic surface
A: hydrophobic surface
Water
Air

## Slide 9
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Hydrophobic (i.e. averse to water or non-wettable) – are substances with greater affinity for air.
Hydrophilic (or water-friendly or wettable) – are substances with greater affinity for water
Only a few minerals are naturally hydrophobic, but several minerals can be made hydrophobic by adsorption of certain chemicals

## Slide 10
5.2. Froth flotation fudamentals (cont.)
MS© 2021

## Slide 11
Criterion for the Spontaneous Adhesion of Air Bubble on Solid Surfaces
5.2. Froth flotation fudamentals (cont.)
MS© 2021
ΔE = after – before = γS/A – (γW/A + γS/W) …(1)
Air
γS/A
Air
γW/A
γS/W
Adhesion
Water
Solid
When ΔE < 0 adhesion occurs.
We can measure γW/A only
disappeared
created
Change of free energy
Solid
γ:surface tension
Before adhesion
After adhesion
Three surfaces
Energy required for adhesion

## Slide 12
Criterion for the Spontaneous Adhesion of Air Bubble on Solid Surfaces (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
The forces tending to separate a particle and a bubble are shown below.
The attachment of the bubbles to the surface is determined by the interfacial energies between the solid, liquid, and solid phases. This is determined by the Young
γS/A = γS/W +γW/A cosθ …(2)
where ϒS/A, ϒS/W and ϒWA are the surface energies between solid-air, solid-water and water-air, respectively. From the figure below θ is the contact angle between the mineral surface and the bubble.
γW/A
Air
Water
Solid
θ
γS/W
γS/A

## Slide 13
Criterion for the Spontaneous Adhesion of Air Bubble on Solid Surfaces (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Substituting Eq. 2 into 1 leads to
ΔE = γS/A - (γW/A + γS/W) = γW/A (cosθ-1）
The above entails that if the contact angle is very small, then the bubble does not attach to the surface, while a very large contact angle results in very strong bubble attachment.
That is, the floatability of a mineral therefore increases with the contact angle; minerals with a high contact angle are said to be aerophilic (hydrophobic), i.e., they have a higher affinity for air than water.
In most cases a contact angle near 90° is sufficient for effective froth flotation.

## Slide 14
Particle-Bubble Contact
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Once the particles are rendered hydrophobic, they must be brought in contact with gas bubbles so that the bubbles can attach to the surface.
If the bubbles and surfaces never come in contact, then no flotation can occur.
Particle-bubble collision is affected by the relative sizes of the particles.
If the bubbles are large relative to the particles, then fluid flowing around the bubbles can sweep the particles past without coming in contact.
It is therefore best if the bubble diameter is comparable to the particle diameter in order to ensure good particle-bubble contact.

## Slide 15
Particle-Bubble Contact (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Bubble
Bubble
Coarse particle
Too fine particle
Bubble
Too coarse particle

## Slide 16
Particle-Bubble Contact (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
PbS
30s
1min
4min
Particle size μm
Recovery
Modeling & simulation of mineral processing systems, p342

## Slide 17
Flotation Reagents
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Although some minerals are naturally hydrophobic, they are rarely suitable for froth flotation and the conditions are not favourable to achieve desired concentration of valuable mineral.
Chemicals are needed both to control the relative hydrophobicities of the mineral particles, and to maintain the proper froth characteristics.
There are therefore many different flotation reagents involved in the froth flotation process, with the selection of reagents depending on the specific mineral mixtures being treated.

## Slide 18
Flotation Reagents (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Collectors
Collectors are reagents that are used to selectively adsorb onto the surfaces of particles.
They form a monolayer on the particle surface that essentially makes a thin film of non-polar hydrophobic hydrocarbons.
For example, if two minerals A and B are hydrophilic, collector ( ) can selectively adsorbs mineral A hence only mineral A becomes hydrophobic. Minerals A and B can be separated by flotation.
A
B
Different surface characteristic of the minerals facilitates selective adsorption!
hydrophobic

## Slide 19
Flotation Reagents (cont.)
5.2. Froth flotation fudamentals (cont.)
MS© 2021
Collectors (cont.)
The collectors greatly increase the contact angle so that bubbles will adhere to the surface.
Selection of the correct collector is critical for an effective separation by froth flotation.
Adsorption mechanisms of collectors onto mineral surface are classified into two types.
I. Chemical adsorption II. Physical Adsorption
Chemical bond
e.g., Anionic collector on positively charged solid surface
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 20
MS© 2021
Collectors/promotors – these are reagents that make certain minerals hydrophobic and thus amenable to flotation.
Frothers – these are reagents that prevent an air bubble from bursting & losing its mineral load when it reaches the surface of the pulp, i.e., bubbles are stabilized with a frother so that a mineralized froth is formed that is sufficiently stable to be separated from the pulp.
Selectivity of collector/mineral adsorption depends on
    pulp pH
    presence of other ions
5.2. Froth flotation fudamentals (cont.)

## Slide 21
MS© 2021
Depressants – prevents the adsorption of a collector on a particular minerals
  Activators – enhances the adsorption
  pH modifiers – controls pulp pH
Nearly, all sulphide minerals are concentrated by flotation.
Oxide minerals (oxides, carbonates, phosphates, silicates etc.,) are difficult to recover by flotation especially if collectors used in sulphidic ores are used.
5.2. Froth flotation fudamentals (cont.)

## Slide 22
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 23
5.3. Jig
MS© 2021
Jigs are normally used to concentrate material of relatively course particle sizes (≥ 1mm) and fairly closed size range (top size to bottom size ≅ 3:1, i.e. 3 – 10mm).
In principle, liberated valuable minerals and gangue particles of different specific gravities, sizes and shapes are fed to the jig chamber.
Particles in a jig chamber are supported by the jig support screen or ragging materials and form a jig bed.
Fluid, usually water for a traditional jig, is vertically pulsated vertically through the bed of particles by either a piston or diaphragm.

## Slide 24
5.3. Jig (cont.)
MS© 2021
Air injection
Release
Separation chamber
Air chamber
Water
Bottom screen
Batac jig
(Settling velocity: slow）
Low SG*
(Settling velocity: fast）
High SG*
Denver jig
Jigs are normally used to concentrate relatively material of course particle sizes (≥ 1mm) and fairly closed size range (top size to bottom size ≅ 3:1, i.e. 3 – 10mm).

## Slide 25
MS© 2021
Source: Mineral processing design and operations an introduction p508
Behaviour of bed, particles and mechanism of stratification of particles
The upward stroke makes the bed to expand (during this stage particles move against gravity) while the downward stroke make the bed to contract (particles fall to the support screen or ragging material due to gravity). This causes stratification.
Dense and course particles, migrate towards the bottom of the jig bed and removed as concentrate.
Jig are widely used in iron ore, tungsten, tin, and coal concentration
5.3. Jig (cont.)

## Slide 26
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 27
5.4. Spiral
MS© 2021
Spiral concentrators consist of a curved-bottom launder which is twisted/turned around a vertical axis in form of a helix.
Slurry, feed material of size range 0.1- 1.5mm, composed of valuable minerals and gangue is fed at the top of the spiral concentrator.
Source: Mineral processing design and operations, p524

## Slide 28
MS© 2021
Less dense minerals particles being suspended in water attain higher tangential velocities than the dense mineral particles, and migrate toward the outer rim of the spiral.
With the help of added wash water, and after many turns, band of dense mineral particles form inside the rim while less dense mineral particles towards the outer rim.
Ports for removal of dense mineral particles are spaced along the inner rim while the less dense mineral particles remains in the spiral and discharges at the bottom.
Spirals are widely used in gold, coal, tungsten, and iron ore concentration.
5.4. Spiral (cont.)

## Slide 29
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 30
5.5. Dense media seperation
MS© 2021
Dense media separation is widely used in upgrading/concentration of iron ore, coal, tin, gold and tungsten.
It operates on the sink-float principle (heavy minerals/materials sink while less dense minerals/materials floats).
Source: Wills, B. A., and Napier-Munn, T., 2005)

## Slide 31
5.5. Dense media seperation (cont.)
MS© 2021
Medium which has a specific gravity (sg) between valuable mineral sg and gangue material sg is mostly prepared by adding finely ground ferro-silicon (15% silicon and 85% iron) in water.
Feed material composed of gangue and valuable mineral particles is added into the vessel containing medium of a given s.g.
For example, silica-rich particles with a specific gravity (s.g 2.6) lower than specific gravity of made media (e.g. s.g 3.0) floats on the surface while the iron rich particles (s.g 4.0) sink to the bottom.
Ferrosilicon is washed from the sink and float products on fine screens and is recovered from the wash water with magnetic separators and recycled.

## Slide 32
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 33
5.6. Dense media seperation
MS© 2021
Magnetic separation is the simple iron ore upgrading/concentration processes that depends on the differences in magnetic properties between iron minerals and gangue minerals.
Source: King, I., 2000 and Will, B.A., and Napier-Munn, T., 2005)
Iron ore
Gangue

## Slide 34
5.6. Dense media seperation (cont.)
MS© 2021
The concentration process is either wet or dry for fine and course particles, respectively.
For less magnetic iron ore, say hematite, High Intensity Magnetic Separators (HIMS) are used, whereas for high magnetic iron ore, say magnetite, Low Intensity Magnetic Separators (LIMS) are used.
Separator consists of a rotating drum and a stationary internal magnet. Magnetic iron ore minerals adhere to the drum as it passes through the suspension of iron ore particles in water.
When the adherent solids are carried out of the magnetic field they are scrapped off the drum and transferred to a receiving vessel.

## Slide 35
5.1. Introduction
5.2. Froth flotation fundamentals
5.3. Jig
5.4. Spiral
5.5. Dense media separator
5.6. Magnetic separator
5.7. Dewatering
Lecture content
MS© 2021

## Slide 36
5.7. Dewatering
MS© 2021
Dewatering is the partial/complete removal of water from a mixture of solids & water.
Dewatering is aimed at:
    Reducing transportation & storage costs
    Reducing the cost of smelting
    Controlling a pulp that may be too dilute for the next treatment step
Here, water is undesirable component & is either discarded or recycled
Industrial filtration requires that a pulp is thickened first using thickeners & hydrocyclones that removes excess water.
Other process steps such as roasting & smelting requires complete drying by evaporation

## Slide 37
5.7. Dewatering
MS© 2021
Thickener to remove excess water
Source:https://www.zerodayllc.com/blog/2015/01/26/thickener-operation/

## Slide 38
5.7. Dewatering
MS© 2021
Filter to remove the remaining water/solution from the thickener underflow
Source:https://www.zerodayllc.com/blog/2015/01/26/thickener-operation/

## Slide 39
Write brief note on copper sulfide concentration by froth flotation
State two mechanisms by which collector adsorbs selectively on surfaces particles
What is the function of frother in mineral concentration by froth flotation
Why do you need to do dewatering of concentrate produced via flotation?
Revision questions

## Slide 40
End of Lecture 5