## Slide 1
GMM 2110: Introduction to Geology Mining and Metallurgy
By
Marthias SILWAMBA (PhD)
Metallurgical Engineering Department
Marthias.silwamba@unza.zm

## Slide 2
Lecture 6
Principles of extractive pyrometallurgy
MS© 2021

## Slide 3
By the end of the lecture students are expected to:-
Understand purpose and principles of pyrometallurgical pretreatment.
Understand basics of sulphide concentrate smelting
Understand basics of oxide concentrate reductive smelting.
Lecture of objective(s)
MS© 2021

## Slide 4
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 5
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 6
Pyrometallurgy is the branch of metallurgy that deals with the use of high temperature to extract metals of interest from mineral/concentrate/metallurgical ore and purification of the extracted metal.
Non-ferrous (i.e., Cu, Ni, Pb etc.,) pyrometallurgy involves the high-temperature extraction and separation of extracted metal via multiple sulfide oxidizing stages.
The smelting process produces three products as below
  Metal of interest is concentrated in one phase (matte or hot metal) until considered sufficiently pure
  Impurities are concentrated in the slag
  Some impurities are expelled as a gas (called off-gas)
6.1. Introduction
MS© 2021

## Slide 7
Slag is molten mixture of metal oxide and silicates.
They are formed in smelting of ores or in the refining of crude metals.
The function of slag is to contain the largely unwanted constituents in the furnace, such as gangue from the ore/concentrate during smelting , and impurity elements oxidized from valuable metal during refining.
Mate is an important intermediate product in Cu and Pb smelting processes.
In sulphide smelting, matte is composed of Cu2S, Ni３S2, FeS containing minor components like PbS, ZnS, Au, and Ag.
In oxide reductive smelting, e.g., Fe-metallurgy, hot metal is the intermediate product.
6.1. Introduction (cont.)
MS© 2021

## Slide 8
Various fluxes are used to:-
    Lower the melting point of slag &
    Improve the fluidity of slag
Fuel used that are are include coke, oil, or natural gas.
Two uses of fuel:-
    Provides the required heat,
    Takes part in the chemical reactions as a reducing agent
6.1. Introduction (cont.)
MS© 2021

## Slide 9
6.1. Introduction (cont.)
CONCENTRATE
PYROMETALLURGY
OXIDE PYROMETALLURGY
SULPHIDE PYROMETALLURY
SLAG
METAL
METAL
TO DUMP
MS© 2021

## Slide 10
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 11
6.2. Pretreatment: Roasting
MS© 2021
Roasting involves changes in chemical composition of ores by the reaction with furnace atmosphere at high temperature (500~1000℃).
Roasting type | 
For sulfide | For oxide
Oxidizing roast | Reduction roast
Sulphation roast | Sulphation roast
Chloridising roast | Chloridising roast

## Slide 12
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 13
6.2.1. Pretreatment: Oxidizing roasting
MS© 2021
Conversion of sulfide to oxide by oxidation.
Dead roasting (complete oxidation) of ZnS, PbS before carbon reduction (or acid leaching of ZnO).
2 ZnS + 3 O2 = 2 ZnO + 2 SO2(g)
Partial roasting of CuFeS2, Ni3S2 before matte smelting
4CuFeS2 + 7O2 = 2Cu2S +FeS +Fe3O4 + 5 SO2(g)
MS
MO
O2
SO2
Heat

## Slide 14
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 15
6.2.2. Pretreatment: Sulphation Roasting
MS© 2021
Conversion of oxide to sulfate prior to hydrometallurgical treatment (sulfate is easier to dissolve in water than oxide).
1/2 O2 (g) + SO2 (g) = SO3(g)
MO (s) + SO3(g) = MSO4 (s)
MO
MSO4
SO3

## Slide 16
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 17
6.2.3. Pretreatment: Reduction roasting
MS© 2021
Conversion of oxide to metal (or reduced oxide)
  NiO + H2 = Ni + H2O
  3 Fe2O3 + CO = 2 Fe3O4 + CO2 (Magnetization for separation)
  2 As2O5 + 2 CO = As2O3 + 2CO2 (Higher volatility to remove)
  MnO2 + CO = MnO + CO2 (Higher leachability)
MO
M or
MOx-1
CO or H2
CO2 or H2O

## Slide 18
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 19
6.2.4. Pretreatment: Chloridising roasting
MS© 2021
Conversion of oxide to volatile chloride
As Cl source, Cl2,NaCl or CaCl2 is used.
MO + Cl2 = MCl2↑ + 1/2O2

## Slide 20
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 21
6.3. Smelting of sulphide concentrate
MS© 2021
Concentrate（20-40%)
Smelting
Blister Cu
（>98.5%)
Cu（>99.99%)
Anode（>99.5%)
Matte
（50-60%)
Electro-refining
Converting
Removal of major impurities (Fe, S）
Removal of minor impurities（O, Pb etc.)
Converting
Fire-refining

## Slide 22
6.3. Smelting of sulphide concentrate (e.g., CuFeS2)
MS© 2021

## Slide 23
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 24
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
MS© 2021
Slag, FeO・SiO2 (acidic slag)
Matte,Cu2S
Instant ignition and melting by exothermal oxidation of Fe and S
Phase separation of Matte and Slag by Specific gravity difference
CuFeS2,SiO2
Removal of Fe in CuFeS2 as slag (FeO・SiO2)
2CuFeS2 + 2SiO2 + 4O2 → Cu2S + 2FeO・SiO2 + 3SO2

## Slide 25
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 26
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
MS© 2021
Removal of S from Matte（Cu2S）
Cu2S + O2 → 2Cu + SO2 （Reduction）

## Slide 27
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 28
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
MS© 2021
The molten blister copper is refined in anode furnaces to anode copper (purity > 99.5％) after oxidation by air blowing and reduction by oil combustion.

## Slide 29
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 30
6.3.4. Smelting of sulphide concentrate: Electro-refining
MS© 2021
Anode Cu → Cu2+ + 2e-
Cathode Cu2+ + 2e- → Cu
High purity Cu (>99.99％) is produced using the redox potential difference !
Anode Cu → Cu2+ + 2e-
Cathode Cu2+ + 2e- → Cu
＋ Anode Cu
－ Cathode Cu
Cu2+
Au
Nobel metals precipitate as slim
Zn2+
Base metals do not plate on cathode

## Slide 31
6.1. Introduction
6.2. Pretreatment: Roasting
6.2.1. Pretreatment: Oxidizing roasting
6.2.2. Pretreatment: Sulphation Roasting
6.2.3. Pretreatment: Reduction roasting
6.2.4. Pretreatment: Chloridising roasting
6.3. Smelting of sulphide concentrate
6.3.1. Smelting of sulphide concentrate: Smelting (Flash Smelting Furnace)
6.3.2. Smelting of sulphide concentrate: Converting (Peirce-Smith Converter)
6.3.3. Smelting of sulphide concentrate: Fire refining and anode casting
6.3.4. Smelting of sulphide concentrate: Electro-refining
6.4. Smelting of oxide concentrate (reductive smelting)
Lecture content
MS© 2021

## Slide 32
4.4. Smelting of oxide concentrate (reductive smelting)
MS© 2021
Reactions:
2C + O2 = 2CO
MO + CO = M + CO2
M: Fe, Pb, Sn etc.
Feed:
Ore (MO + SiO2, Al2O3 etc)
Cokes (C)
Flux (CaO)
Products:
Crude Metal + Slag (basic slag)

## Slide 33
6.4. Smelting of oxide concentrate (reductive smelting) (cont.)
MS© 2021
In Blast furnaces
  The charge or burden i.e. ore/concentrate/roast calcine, fuels & fluxes are charged from top
  pre-heated air (blast) is blown in from the bottom
An iron blast furnace produces a slag & an impure Pig Iron.
A lead blast furnace produces a slag & an impure lead bullion.
Common fluxes are silica (in copper smelting) as well as limestone & dolomite (used in Fe & steelmaking).
Slags can be acidic (high in SiO2) or basic (high in CaO & MgO).

## Slide 34
6.4. Smelting of oxide concentrate (reductive smelting) (cont.)
MS© 2021
Reduction Smelting of Iron oxide ore/mineral in Blast Furnace
CO
CO2
Fe2O3
FeO3–y

## Slide 35
End of Lecture 6