## Slide 1
MET 2419: Introduction to Mineral Sciences
By
Marthias SILWAMBA (PhD)
Metallurgical Engineering Department
Marthias.silwamba@unza.zm

## Slide 2
Lecture 7
Principles of extractive hyrometallurgy
MS© 2021

## Slide 3
By the end of the lecture students are expected to:-
Understand principles of hydrometallurgical processes.
Understand basics principle of pregnant solution purification/concentration
Understand basics of valuable metal recovery from pregnant solution.
Lecture of objective(s)
MS© 2021

## Slide 4
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 5
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 6
7.1. Introduction
MS© 2021
Hydrometallurgy is a brunch of extractive metallurgy using aqueous chemistry.
Metals are extracted from solid phase (ores, concentrates, and recycled materials) to aqueous solution, then the extracted metal ions are recovered as a solid materials by reduction or precipitation.
MO, MS
Mn+
Precipitation or Reduction
M, MX
Leaching

## Slide 7
7.1. Introduction (cont.)
MS© 2021
Leaching
Purification
Metals in ore are extracted as ions in aqueous phase.
Valuable product of leaching is called pregnant solution. It is separated from insoluble leach residue by thickening, followed by filtration.
Concentration of valuable mineral and removal of impurity (ex. Fe）from aqueous phase.
Solution purification & concentration can be done by chemical precipitation but more often by ion exchange.
Metal ions in aq. are recovered by reduction or precipitation
Metal recovery can be done by chemical precipitation as a compound or by electrolytic (electrowinning) and reductive precipitation (i.e., cementation and H2 reduction).
Heap Leaching
Solvent Extraction
Electro Winning
Recovery
e.g.,
e.g.,
e.g.,
General Outline of Hydrometallurgical Processes

## Slide 8
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 9
7.2. Leaching of ore/concentrate
MS© 2021
Men+
Men+
  Leaching is the first step of hydrometallurgical processes
  Valuable metal ions are ‘selectively’ extracted from solid ore or mineral to leachate (aqueous solutions), and non valuable matter are remained in solid residue.
  In real process, gangue elements co-dissolve during leaching and these are removed during purification stage.

## Slide 10
MS© 2021
Leaching methods
Method | Unit size | Extraction time | Yield | Particle size | Control | Cost
In-situ | > 106 t | Years | low | Fractured | low | low
Dump | > 105 t | Med.years | low | Fractured | low | low
Heap | > 104 t | Months | low | Crushed | low | low
Vat | > 103 t | Days | medium | Crushed | low | medium
Agitation | > 102 t | Hours | High | Ground fine | high | high
Pressure | > 10 t | Minutes | High | Ground fine | high | high
7.2. Leaching of ore/concentrate (cont.)

## Slide 11
MS© 2021
Several solvents (lixiviants) may be used but sulphuric acid is more common
Sulphuric acid is widely used since
[1] it is cheap (often produced as a by-product)
[2] it can be regenerated
However, sulphuric acid is corrosive and not selective (leaches too many metals), so purification of leach solution is often necessary.
Ammonia is less corrosive but more selective and is used in several applications in preference to sulphuric acid. Its more expensive but can be regenerated & remainder often used as a fertilizer
NaOH is the only lixiviant used to leach bauxite. NaCN is the only lixiviant used to leach gold ores
7.2. Leaching of ore/concentrate (cont.)

## Slide 12
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 13
7.2.1. Heap leaching
MS© 2021
Large heaps of low-grade are placed on previously prepared impervious pads.
The lixiviant is sprayed on the heaps with a system of pipes and trickles (percolates) through the ore, dissolving the metal on its way

## Slide 14
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 15
7.2.2. In-situ leaching
MS© 2021
Lixiviant is introduced from the surface to just above the level of the underground orebody and percolates through the broken ore.
The resulting pregnant solution is very impure. The method is used in some worked out mines containing already broken rocks
Source: http://www.infinitpipe.com/solution-mining.htm

## Slide 16
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 17
7.2.3. Agitation leaching
MS© 2021
Leaching is done in mechanically agitated tanks with impellers or in air-agitated tanks (pachucas).
Particles of concentrates, roast calcines are mixed with lixiviants and kept in suspension by agitation
Source: http://www.infinitpipe.com/solution-mining.htm
Men+
Men+

## Slide 18
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 19
7.3. Lechate Purification and concentration
MS© 2021
Due to impurities that solubilize with the desired metal in solution;
  These impurities can be removed from the solution or
  The valuable metal can be transferred to another solution, leaving the impurities behind
Metals can be removed from solution by precipitation or ion exchange

## Slide 20
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 21
7.3.1. Precipitation
MS© 2021
Precipitation
Because different metal hydroxides have different solubility products, they will precipitate at different pH and a fairly selective precipitation is possible.
Ca(OH)2, i.e., lime, is cheap and therefore most commonly used for raising pH and effecting such selective precipitation.
Fe3+ can easily be separated from Cu2+

## Slide 22
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 23
7.3.2. Ion exchange
MS© 2021
Ion Exchange
An extractant is used that is selective for a particular metal ion. Here extractant is contacted with a solution of the desired metal under suitable conditions;
The metal joins the extractant in exchange for another type of ion that moves into solution. This is the extraction or loading or sorption
Loaded extractant is next contacted with an eluent or strip solution under different conditions.

## Slide 24
7.3.2. Ion exchange (cont..)
MS© 2021
This drives the metal ion out of the extractant into the strip solution in exchange for another ion from this solution
ion exchange methods include
  ion exchange using solid exchange resins
  ion exchange using activated charcoal
  liquid-liquid ion exchange or Solvent Exchange
Solvent Extraction was successfully developed for the extraction of copper

## Slide 25
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 26
7.3.3. Solvent extraction
MS© 2021
Solvent Extraction
SX (or SEX) uses a liquid extractant that is immiscible with an aqueous solution.
The extractant is dissolved in an organic diluent (e.g.kerosene), also immiscible with an aqueous solution.
This gives about equal proportions of the organic & aqueous phases such that vigorous agitation will give good contacting of the two phases
The phases are allowed settle so that they can disengage;
  Barren solution is called raffinate & is recycled to the leach circuit.
  The loaded organic proceeds to the stripping circuit

## Slide 27
7.3.3. Solvent extraction (cont..)
MS© 2021
Solvent
(light phase)
Aqueous
(heavy phase)
Well dispersed organic solvent in aqueous phase
Well dispersed organic solvent in aqueous phase
Extractant
Target metal ions
Other metal ions

## Slide 28
7.3.3. Solvent extraction (cont..)
MS© 2021
Equilibrium reaction is given by;
RHn + Men+ = RMe + 2H+ where R = organic extractant
(Organic) (Aqueous) (Organic) (Aqueous)
Equilibrium depends on pH;
[1] At relatively high pH (low H+ ion concentration), the reaction proceeds to the right ( extraction)
[2] At low pH (high H+ ion concentration), reaction proceeds to the left (stripping)

## Slide 29
7.1. Introduction
7.2. Leaching of ore/concentrate
7.2.1. Heap leaching
7.2.2. In-situ leaching
7.2.3. Agitation leaching
7.3. Lechate Purification and concentration
7.3.1. Precipitation
7.3.2. Ion exchange
7.3.3. Solvent extraction
7.4. Metal recovery from the pregnant leach solution
Lecture content
MS© 2021

## Slide 30
MS© 2021
1. Cementation
Metals dissolved in solution can be precipitated by solid metals that have a lower reduction potential (higher oxidation potential)
Metal with a higher oxidation potential goes into solution and the more noble metal precipitates out
Fe = Fe2+ + 2e- (oxidation)
Cu2+ + 2e- = Cu (reduction)
--------------------------------------------------------------
Cu2+ + Fe = Cu + Fe2+ (overall reaction)
Cementation is widely used to recover copper cheaply from impure & dilute leach solutions
Mles
e-
e-
MeXm
n–
Mles
n+
7.4. Metal recovery from the pregnant leach solution

## Slide 31
MS© 2021
2. Electrowinning
Metals dissolved in the electrolyte are made to precipitate onto the cathode while the anode is inert
Electric current carries metal cations to the cathodes where they discharge & precipitate onto the cathodes as pure metal
Anode reactions are different for each process. In general, water is dissociated to give to oxygen
e.g Cathode rxn: Cu2+ + 2e- = Cu
Anode rxn: H2O = H+ + OH- = ½ O2 + 2H+ + 2e-
----------------------------------------------------------------------------------------------------------------------------------------
Overall: Cu2+ + H2O = Cu + ½ O2 + 2H+
Mass of metal deposited at the cathode is proportional to the quantity of electricity passed (current density)
Current efficiency = actual mass of metal deposited divided by the theoretical amount, this is about 75 -95 %. Current losses occur due to short circuits, resistances etc.
7.4. Metal recovery from the pregnant leach solution (cont..)

## Slide 32
MS© 2021
7.4. Metal recovery from the pregnant leach solution (cont..)
Electrorefining
Electrowinning
Difference between electrorefining and electrowinning

## Slide 33
End of Lecture 7