MI 315:  ROCK MECHANICS LAB NO. 2A

DETERMINATION OF UNIAXIAL COMPRESSIVE STRENGTH OF ROCK SPECIMENS BY DIRECT METHOD

- Scope

This test measures the Uniaxial Compressive Strength of cylindrical rock specimens for strength clarification and characterization of intack rock.

- Specimens

Specimens should have been adequately prepared and having a height to diameter to meet the specifications of the

- Apparatus

A suitable machine shall be used for applying and measuring axial load to the specimen.  It shall be of sufficient capacity and capable of applying load as a constant rate.  In our lab, the Universal Testing Machine shall be used for this purpose.

- Procedure

- Ensure that the machine’s dial gauge is at zero.

- Place the specimen on the centre of the Universal testing machine platens.

- Load the specimen continuously at a constant rate such that failure will occur within 5-10 mins. Of load Alternatively, the stress rate should be within 0.5-1.0 MPa/s.

- Record the load at failure as failure load (P) in Newton.

- Clean the platens and repeat procedure (i)-(iv) for other specimens.

- Calculations

The Uniaxial Compressive Strength of the specimen (Qu) shall be calculated by dividing the maximum load carried by the specimen during the test (P) by the original cross-sectional area.

- Assignment

Prepare a lab report and determine the average Uniaxial Compressive Strength of the rock specimens tested.  Briefly explain why the load on the specimen should be applied continuously at a constant stress rate.

DETERMINATION OF UNCONFINED COMPRESSIVE STRENGTH

Note

- Method is intended to measure Compressive Strength of rock samples of regular geometry.

- The samples can be cut from diamond drill cores from exploration drilling or core drilled in the lab from blocks of rock selected from areas of interest.

- The test is mainly intended for rock strength classifications.

Also to be noted are:

Specimen requirements

1.	Test specimen should be right circular cylinder.  Length of samples are usually longer than its dia (2-3) i.e. L/D ratio.

2.	The ends of the specimen should be flat to 0.02 mm (mm).

3.	The sides of the specimen should be smooth and straight to within 0.3 mm over the full length.

4.	No. of samples to be tested should preferably not be less than 5.

5.	Load on the specimen should be applied continuously at a rate of 0.5-1.0 minutes or 5 to 10 minutes.

DIAGRAM

Note that:  Most of the mentioned requirements have to be done in the lab.  Prior to specimen testing there is a specific practical or called sample preparation.

This involves, Core drilling, cutting and polishing.

We all know:  What Compression is

Platen

Mathematically:

Compressive Strength =  _Failure load (N)    =    MPa

X/Sec Area (mm2)

Correction

Tabulate the results

| Sample No | Failure Load (Kg) | Press (Force) or Weight Kg x 9.81 N | Dia Mm | x/sec Area Mm2 | Comp. Strength After MPa |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 19500 |  | 50 |  |  |  |
| 2 | 21200 |  |  |  |  |  |
| 3 | 20000 |  |  |  |  |  |
| 4 | 27000 |  | 63 |  |  |  |
| 5 | 25000 |  | “ |  |  |  |
| 6 | 24000 |  | “ |  |  |  |

Average Compressive Str   1 + 2 +_ 3 + 4

4

ROCK MECHANICS LABORTORY NO 3

DETRMINATION OF TENSILE STRENGTH OF ROCKS BY THE BRAZILIAN METHOD (INDIRECT METHOD)

SCOPE

This test measures the Uniaxial Tensile Strength of prepared cylindrical rock specimens indirectly by the Brazilian method for strength classification and characterization of intact rock.

Specimens

The specified no. of specimens should both adequately prepared to meet the specifications of the ISRM i.e. D/L = 1: 0.5 or NX

Apparatus

- An apparatus for Brazil test, two steel loading jaws designed so as to contact a disc shaped rock specimen at diametrically-opposed surfaces over an arc of approximately 100 at failure.

- A Compressive Testing Machine is able to apply and measure axial loads such that the primary failure can be measured precisely.  Universal Testing Machine.

Procedure

- Place specimen diametrically between the loading machine platen

- Apply a load on the specimen continuously at a constant rate of approximately 200N/s until failure occurs.

- Record the ultimate failure load, P (in Newtons)

- Clean the apparatus and repeat procedure for the remaining specimens

Calculations

The Tensile Strength of the specimen a2 shall be calculated as follows;

- a2 = 0.636 P/Dt (MPa)

OR

- a2  = 2P/xDt			where P is the failure load (N)

D is the specimen diameter (mm)

T is the specimen thickness (mm)

Assignment

Write a brief lab report and determine av. Tensile strength of the rock specimens tested.

Compressive Strength Data

- 24,200 Kg

- 19,250

- 24,700

- 24,750

- 21,300

____________________________________

Tensile Data

- 3,850 kg

- 4,500

- 3,200

- 4,200

- 3,900